## Slide 1
4.33 MECHANICAL PROPERTIES OF WOOD
Because of its structure, wood has different strength properties parallel and perpendicular to the grain. Tensile, bending, and compressive strengths are greatest
parallel to the grain and least across the grain, whereas shear strength is least
parallel to the grain and greatest across the grain. Except in plywood, the shearing
strength of wood is usually governed by the parallel-to-grain direction.
Lumber is graded by the various associations of lumber manufacturers having jurisdiction
over various species. Two principal sets of grading rules are employed:
(1) for softwoods, and (2) for hardwoods.
Softwoods. Softwood lumber is classified as dry, moisture content 19% or less;
and green, moisture content above 19%.
According to the American Softwood Lumber Standard, softwoods are classified
according to use as:
Yard Lumber. Lumber of grades, sizes, and patterns generally intended for ordinary
construction and general building purposes.
Structural Lumber. Lumber 2 in or more nominal thickness and width for use
where working stresses are required.
Factory and Shop Lumber. Lumber produced or selected primarily for manufacturing purposes.
Softwoods are classified according to extent of manufacture as:
Rough Lumber. Lumber that has not been dressed (surfaced) but has been
sawed, edged, and trimmed.
Dressed (Surfaced) Lumber. Lumber that has been dressed by a planning machine
(for the purpose of attaining smoothness of surface and uniformity of size)
on one side (S1S), two sides (S2S), one edge (S1E), two edges (S2E), or a combination
of sides and edges (S1S1E, S1S2, S2S1E, S4S).
Worked Lumber. Lumber that, in addition to being dressed, has been matched,
shiplapped or patterned:
Matched Lumber. Lumber that has been worked with a tongue on one edge of each piece and a groove on the opposite edge.