## Slide 1
12.3 ROOF INSULATION
Many of the insulation products described in the following are available in tapered configurations.
Cellular glass is a rigid insulation composed of heat-fused closed glass cells.
Cellulosic fibers are generally used as loose-fill insulation. They are made of recycled paper.
Glass-fiber batts or blankets (the only difference being the length of the prod- uct) are composed of glass fibers and a binding agent. The batts may be finished on one side with a kraft paper or aluminum-foil facer, or they may be left unfaced.
Glass-fiber board is a rigid insulation composed of glass fibers and a binding agent and is faced on the top surface with kraft paper.
Mineral-wool batts are similar to glass-fiber batts, except that they are com- posed of mineral fibers (produced from molten rock). Mineral-wool batts have high resistance to heat. Typically, they are used for fire-safing; for example, curtain walls or sealing at fire wall or floor penetrations, or steel fireproofing. Mineral batts are typically not used for roofing, except for insulating seismic joints or expansion joints, where enhanced fire resistance is desired.
Mineral-wool board is a rigid insulation similar to glass fiber boards except that it is composed of mineral fibers (produced from molten rock). These boards are available faced or unfaced with aluminum foil.
Perlite rigid insulation is composed of expanded perlite, cellulose, and a binding agent.
Phenolic resin has been formed into a rigid, plastic-foam insulation. It is no longer produced in the United States. It should be noted that phenolic insulation has shown a high potential for causing steel deck corrosion, and in some instances, the structural integrity of the roof deck has been impaired. Deck repair or replace- ment should be anticipated where phenolic insulation over a steel deck exists.