## Slide 1
L
UEENEEG101A Solve problems in electromagnetic devices and related circuits
Magnetisation Curves
Notes: Title

## Slide 2
Objectives
At the end of this section students should be able to:
1. Describe and draw typical magnetisation curves.
2. Describe and draw typical Hysteresis curves.
3. Describe the meanings of the terms Saturation, Hysteresis, and Losses in magnetic circuits.
4. Compare the magnetic characteristics of a number of materials.
5. Describe Magnetic Losses and their effect on the performance of electrical machines.
L

## Slide 3
Φ = Flux in Webers
h
w
Area = width x height
A = Area in m2
B = Flux Density
What is Flux Density?
L

## Slide 4
d
d
Area = πr2 = π(d/2)2
A = Area in m2
Φ = Flux in Webers
B = Flux Density
What is Flux Density?
L

## Slide 5
Magnetic Flux Density (B) in the core of a magnetic circuit is dependent on the Permeability (μ) of the core and the Magnetising Force (H).
The SI Unit of Flux Density is the Tesla (B)
1 Wb/m2 = 1 Tesla
H = Magnetising Force
μ = Permeability
B = Flux Density
L

## Slide 6
Magnetising Force (H) [At/m]
Flux Density (B) [Tesla]
Air
Magnetisation Curves
Cast Iron
Cast Steel
Silicon Steel
L

## Slide 7
Magnetising Force (H) [At/m]
Flux Density (B) [Tesla]
Non – Magnetic Material
Magnetisation Curves
Magnetic Material
Saturation
Reasonably Linear Operating Region
Knee
L

## Slide 8
Find the Magnetising Force (H) necessary to produce a Flux Density of 0.75 T in a 300 mm Cast Steel Toroidal core from a coil with 500 turns.
l = 300 mm
N = 500 turns
Cast Steel
B = 0.75T
L

## Slide 9
Given:
l = 300 mm
N = 500 turns
Cast Steel
From Magnetisation (B/H) Curves
For: B = 0.75 T
B = 0.75 T
H = 750 At/m
L

## Slide 10
Find the Magnetising Force (H) necessary to produce a Flux Density of 0.75 T in a 300 mm Cast Iron Toroidal core from a coil with 500 turns.
l = 300 mm
N = 500 turns
Cast Iron
B = 0.75 T
L

## Slide 11
Given:
l = 300 mm
N = 500 turns
Cast Iron
From Magnetisation (B/H) Curves
For: B = 0.75 T
B = 0.75 T
H = 4 500 At/m
L

## Slide 12
+H
-H
+B
-B
Residual Magnetism
Coercive Force
B-H Curves
Saturation
Saturation
Hysteresis Curve
L

## Slide 13
L

## Slide 14
Practical Exercise 4
The Magnatisation Curve
L